## Slide 1
Andrzej Ożarowski, National High Magnetic Field Laboratory, Florida State University
High‒Field EPR Studies on Polynuclear Transition Metal Complexes
Wrocław, 8 września 2025

## Slide 2: Why High‒Field EPR? Is X‒Band insufficient?
DPPH is a stable free radical used often as an EPR standard. Its X‒Band frozen solution spectrum suggests that the g tensor is isotropic and giso= 2.004. 5‒line hyperfine structure due to 2 nitrogen nuclei is seen.
Wrocław, 8 września 2025

## Slide 3: Why High‒Field EPR? Is X‒Band insufficient?
A 406.4 GHz spectrum shows 3 g components The distance between gx and gz is 145 Gauss, but at the X‒Band frequency of 9.6 GHz it is 3.4 G and the g components are not resolved.
Wrocław, 8 września 2025

## Slide 4: Why High‒Field EPR? Is X‒Band insufficient?
[Zn1–xNix(HF2)(pyz)2]SbF6 (x = 0.2; pyz = pyrazine) J. Am. Chem. Soc. 2021, 143, 12, 4633–4638.
Wrocław, 8 września 2025
gx = 2.238 gy = 2.250 gz = 2.144
D = +11.193 cm‒1, E = 0

## Slide 5
THE SIGN OF D
The EPR resonance fields do not depend on the sign of D (or E). With D positive, a Z transition at ~4T starts from the ground state. With D negative, it starts from an excited state resulting in a different intensity pattern at sufficiently low temperatures, where the Zeeman energy is comparable to the thermal energy kT.
D = +11.193 cm‒1
D = ‒11.193 cm‒1

## Slide 6
THE SIGN OF D (S=1)
gx = gy | gz | D, cm‒1 | E, cm‒1
2.063 | 2.318 | ‒1.140 | ‒0.0393

## Slide 7: EXCHANGE INTERACTIONS
The paramagnetic metal ions in polynuclear complexes may interact directly “through space”, or indirectly through the ligands bridging them. This so‒called exchange interaction is an electrostatic effect, but it may be described in terms of the Heisenberg‒Dirac‒VanVleck Hamiltonian which uses only the spin operators. For a binuclear complex of metal ions with spins S1 and S2, this interaction couples the two spins to produce the total spin states with the S quantum numbers over a range|S1‒S2| to S1+S2. The energies are
Wrocław, 8 września 2025
Energy levels in a Binuclear Iron(III) Complex
Energy [J]
‒8
‒6
‒4
‒2
0
2
4
6
S = 0
S = 5
S = 1
S = 4
S = 2
S = 3

## Slide 8: COPPER ACETATE The first binuclear complex ever studied by EPR
Wrocław, 8 września 2025
“Anomalous Paramagnetism of Copper Acetate” B. Bleaney, K. D. Bowers Proc. Roy. Soc. London, Series A, 214, 451 (1952)

## Slide 9: X‒BAND SPECTRA OF THE EXCITED S=1 STATE

## Slide 10: HIGH‒FIELD SPECTRA OF THE EXCITED S=1 STATE

## Slide 11: HIGH‒FIELD SPECTRA OF THE EXCITED S=1 STATE
Ozarowski, A., The Zero‒Field‒Splitting Parameter D in Binuclear Copper(II) Carboxylates Is Negative, Inorg. Chem., 47 (21), 9760‒9762 (2008)
Cu
Cu
Pyrazinate: gx = 2.0608(2), gy = 2.0622(2), gz = 2.3493(3), D = ‒ 0.328(1) cm-1, E = 0.000(1) cm-1
Hydrate: gx = 2.0545(3), gy = 2.0792(2), gz = 2.3637(2), D = ‒ 0.335(1) cm-1, E = ‒ 0.0103(1) cm-1
80 K

## Slide 12: The Origin of the Zero‒Field Splitting in Copper(II) Dimers
Ĥ = μBB·{g}·Ŝ + D { Ŝz2 ‒ S (S+1)/3 } + E ( Ŝx2 ‒ Ŝy2 )
D = Dex + Ddipole‒dipole
E = Eex + Edipole‒dipole
The experimental D in copper acetate when determined from the X‒Band EPR was 0.34 cm‒1. The sign was unknown but was widely thought to be positive.
The dipolar part of D can be estimated using the Cu‒Cu distance R=2.61 A:
If D is positive, then Dex = +0.50 cm‒1. If D is negative, then Dex = ‒0.18 cm‒1.

## Slide 13: HIGH‒FIELD SINGLE ‒ CRYSTAL SPECTRA (pyrazinate)

## Slide 14: Copper Acetate Monohydrate: 2 Symmetry Related Molecules

## Slide 15: Despite all efforts, the sign of the axial ZFS parameter of the triplet state has only been experimentally determined in 2008.10 High‒field high‒frequency electron paramagnetic resonance (HF‒EPR) spectroscopy was used to unambiguously extract the small ZFS parameters of the thermally accessible triplet state. D was finally found to be negative, at variance with all previous results extracted from experiments all of which relied on the original analytical expressions put forward by Bleaney and Bowers.

## Slide 16: Orbital Interactions

## Slide 17: Orbital Interactions in Cu‒Carboxylates
Maurice, R. ; Neese, F.; et al, Inorg. Chem. 2011, 50, 6229–6236
Orbital Interactions

## Slide 19: Alkoxo ‒ Bridged Copper(II) Complexes
Ozarowski, A., et al., Inorg. Chem., 2015, 54, 11916
[Cu(H2TEA)(CH3O‒C6H4‒COO)]2

## Slide 20: [Cu(CH3O‒C6H4COO)H2TEA]2
R | J, cm‒1 | gx = gy | gz | D, cm‒1 | E, cm‒1 | Dex, cm‒1 | Eex, cm‒1
m‒OCH3C6H4 | ‒101 | 2.064 | 2.311 | ‒1.066 | ‒0.0393 | ‒1.13 | 0.01
o‒OCH3C6H4 | 83 | 2.064 | 2.291 | ‒0.907 | ‒0.0495 | ‒0.97 | 0
p‒OCH3C6H4 | ‒101 | 2.063 | 2.318 | ‒1.140 | ‒0.0393 | ‒1.20 | 0.01

## Slide 21
THE SIGN OF D (p‒methoxy complex)
gx = gy | gz | D, cm‒1 | E, cm‒1
2.063 | 2.318 | ‒1.140 | ‒0.0393

## Slide 22: Orbital Interactions
Formulas taken from Maurice, R. et al., Inorg. Chem. 2011, 50, 6229
(derived for copper acetate)

## Slide 23: Features of the ZFS
Dex and total D are negative.
Dzz(ex) is roughly perpendicular to Dzz(dip). The E parameter is mainly of dipolar origin. For the 2.9 A Cu‒Cu distance one can calculate E = 0.05 cm‒1 without taking the electron delocalization into account, while the experimental magnitudes are 0.04 to 0.05 cm‒1.
In the binuclear copper carboxylates Dzz(ex) is parallel to Dzz(dip) resulting in very small E, typically 0 ≤ E < D / 30

## Slide 24
Binuclear Oxygen‒Bridged Fe(III) Complexes
Ozarowski, A., High–Field EPR Studies on Three Binuclear μ–Oxo–Bridged Iron(III) Complexes: Na4[Fe(edta)]2O ⋅ 3H2O, [Fe(phen)2(H2O)]2O(NO3)4 ⋅ 5H2O and [Fe(salen)]2O
European Journal of Inorganic Chemistry, 2024 (e202400565), 1-9 https://doi.org/10.1002/ejic.20240056
J = 198 cm-1 J = 220 cm-1 J = 174 cm-1
Angle FeOFe 163 155 145

## Slide 25
H=JS1S2
Binuclear Oxygen‒Bridged Fe(III) Complexes

## Slide 26
H=JS1S2
Binuclear Oxygen‒Bridged Fe(III) Complexes

## Slide 27: X‒Band EPR Spectra of [Fe(phen)2(H2O)]2O(NO3)4·5H2O Inorganic Chemistry, 34, 5558‒5566 (1995)
Single Crystal Powder
Spectra of spin state S=2 were observed with giso = 2, D = 0.26 cm‒1, E = 0.037 cm‒1. Resonances of S=3 were also present.

## Slide 28: HFEPR Spectra of [Fe(phen)2(H2O)]2O(NO3)4·5H2O European Journal of Inorganic Chemistry, 2024 (e202400565)
 | gx | gy | gz | D1, cm–1 | E1, cm–1
300 K, S=1 | 2.013(1) | 2.013(1) | 2.003(1) | 4.776(1) | 0.359(1)
The “giant spin” approach
ĤS = μBB·{g}·Ŝ +DS { Ŝz2‒S(S+1)/3 } + ES (Ŝx2‒ Ŝy2)
Each spin state S has its own g matrix as well as D and E

## Slide 29
↔
The transition from one Hamiltonian to the other is accomplished by using the coefficients aS and bS:
DS = aS D12 + bS (DFe1 + DFe2) D12 = Ddipole‒dipole + Dexchange
ES = aS E12 + bS (EFe1 + EFe2) E12 = Edipole‒dipole + Eexchange
+
ĤS = DS { Ŝz2‒S(S+1)/3 } + ES (Ŝx2‒ Ŝy2)
Each spin state has its own g matrix as well as D and E

## Slide 30: Fitting the frequency dependencies
S = 1 S = 2 S = 3

## Slide 31: HFEPR Spectra of [Fe(phen)2(H2O)]2O(NO3)4·5H2O European Journal of Inorganic Chemistry, 2024 (e202400565)
Temperature and spin state | gx | gy | gz | D, cm–1 | E, cm–1
300 K, S=1 300 K, S=2 300 K, S=3 150 K S=1 | 2.013(1) 2.012(1) 2.012(1) 2.013(1) | 2.013(1) 2.012(1) 2.010(1) 2.013(1) | 2.003(1) 2.003(1) 2.004(1) 2.003(1) | 4.776(1) 0.259(1) 0.686(1) 4.645(1) | 0.359(1) 0.036(1) 0.0084(3) 0.374(2)
The “giant spin” approach
ĤS = μBB·{g}·Ŝ +DS { Ŝz2‒S(S+1)/3 } + ES (Ŝx2‒ Ŝy2)
Each spin state S has its own g matrix as well as D and E
Energy levels calculation requires diagonalization of complex matrices 3x3, 5x5 and 7x7 for S=1, S=2 and S=3, respectively.

## Slide 32: Simulation Using the Microscopic Spin Hamiltonian
J=190 cm–1, DFe= –1.462 cm–1, EFe= –0.025 cm–1, D12= –1.242 cm–1, E12= –0.140 cm–1
Diagonalization of 36 x 36 complex matrices was required

## Slide 33: [Fe(salen)]2O
308 K, S=1 308 K, S=2 308 K, S=3 150K, S=1 150 K, S=2 | gx 2.010(1) 2.003(2) – 2.011(2) 2.006(1) | gy 2.012(1) 2.005(1) – 2.009(2) 2.006(1) | gz 2.000(2) 2.006(1) 2.002(1) 2.021(4) 2.002(1) | D, cm–1 10.106(2) 0.689(1) 0.458(2) 10.255(1) 0.738(6) | E, cm–1 1.694(2) 0.223(1) – 1.816(1) 0.218(2)

## Slide 34: [Fe(salen)]2O
308 K, S=1 308 K, S=2 308 K, S=3 150K, S=1 150 K, S=2 | gx 2.010(1) 2.003(2) – 2.011(2) 2.006(1) | gy 2.012(1) 2.005(1) – 2.009(2) 2.006(1) | gz 2.000(2) 2.006(1) 2.002(1) 2.021(4) 2.002(1) | D, cm–1 10.106(2) 0.689(1) 0.458(2) 10.255(1) 0.738(6) | E, cm–1 1.694(2) 0.223(1) – 1.816(1) 0.218(2)

## Slide 35: [Fe(salen)]2O vs. [Fe(salen)]2O CH2Cl2
 | gx | gy | gz | D, cm–1 | E, cm–1
[Fe(salen)]2O 150K, S=1 | 2.011(2) | 2.009(2) | 2.021(4) | 10.255(1) | 1.816(1)
[Fe(salen)]2O∙CH2Cl2* 150K S=1 | 2.008(2) | 2.011(2) | 2.001(7) | 10.924(4) | 0.644(4)
*P. Coggon et al., J. Chem. Soc. (A) 1971, 1014: reported D = 2 cm-1 for both spin states S=1 and S=2

## Slide 36
THE HEXANUCLEAR COMPLEX Mn6{OK(THF)}4(OH)4(pinF)6
The THF molecules and K atoms were omitted for clarity.
Mn(III)
Mn(IV)
C
F
O
(pinF)2‒

## Slide 37
The molecule has a S4 axis passing through the Mn(IV) atoms (marked in brown).
The Mn(III) atoms (blue) lie in a ring perpendicular to the S4 axis.
All 4 Mn(III) ions are equivalent, and the 2 Mn(IV) atoms are equivalent.
The asymmetric unit contains just 1 Mn(III) and 1 Mn(IV). Applying the S4 operation
{y‒1/4, ‒x+5/4, ‒z+5/4}
to the asymmetric unit 3 times generates the entire hexanuclear molecule.
THE Mn6 SKELETON IN Mn6{OK(THF)}4(OH)4(pinF)6

## Slide 38
POSSIBLE EXCHANGE INTERACTIONS
All in‒plane interactions (1‒2, 2‒3, 3‒4 and 4‒1 are equal, according to the symmetry.
Interactions 5‒1, 5‒3 and 6‒2, 6‒4 (are equal.
Interactions 5‒2, 5‒4 and 6‒1, 6‒3 (are also equal but may be different from (
+

## Slide 39
The maximum possible spin is S = 11: 4*2 + 2*(3/2)
There are (54*42) = 10000 microstates |m1 m2 m3 m4 m5 m6 > of the coupled system. They are arranged in 1196 states of the total spin,
ENERGY LEVELS IN Mn6{OK(THF)}4(OH)4(pinF)6
ST | Number of states | Multiplicity (2ST+1)*Number of states
11 | 1 | 23
10 | 5 | 105
9 | 15 | 285
8 | 35 | 595
7 | 68 | 1020
6 | 112 | 1456
5 | 160 | 1760
4 | 200 | 1800
3 | 216 | 1512
2 | 196 | 980
1 | 138 | 414
0 | 50 | 50
Total | 1196 | 10000

## Slide 40
MAGNETIC PROPERTIES OF Mn6{OK(THF)}4(OH)4(pinF)6
= C

## Slide 41
When fitting the magnetic data, we obtain
g = 2.02, A = ‒ 24.4 cm‒1, B = ‒ 4.0 cm‒1.
E(ST, MS) = E(ST) + gbBMS
THE MAGNETIC PROPERTIES

## Slide 42
The fitting procedure gives the exchange integrals A= ‒ 24.4 cm‒1 (4 interactions in the equatorial ring) and B = ‒ 4 cm‒1 (8 ring to vertices interactions).
With these A and B, the ground state is S = 11.
The lowest excited states are S = 10 at 32 and 44 cm‒1, then S = 9 at 64, 72 and 82 cm‒1. However, the errors in A and B may be large.
The ground state is thus reasonably isolated and at low temperature only resonances within the ground S = 11 state should be observed in EPR.
THE SPIN STATES IN Mn6{OK(THF)}4(OH)4(pinF)6

## Slide 43
HFEPR SPECTRA OF Mn6{OK(THF)}4(OH)4(pinF)6

## Slide 44
HFEPR SPECTRA OF [Mn6{OK(THF)}4(OH)4(pinF)6
3
4
5
6
7
8
9
10
Crystal
Q
=10.5o
Powder
30 K, 218 GHz
Magnetic Induction, Tesla

## Slide 45
SINGLE‒CRYSTAL HFEPR SPECTRA (Close to the Z orientation)
2
1
3
6
4
5
8
9
7
10
14
12
11
13
15
22
18
20
16
19
21
17
5
6
7
8
9
10
30 K, 218 GHz
120 K, 218 GHz
Magnetic Induction, Tesla

## Slide 46
gx = 1.935 gy = 1.939 gz = 1.990
D= ‒ 0.0970 cm‒1, E = 0
B40 = ‒ 3.7 10‒6 cm‒1, B44 = 4.3 10‒5 cm‒1
+

## Slide 47
+
gx = 1.935 gy = 1.939 gz = 1.990
D= ‒ 0.0970 cm‒1, E = ‒ 0.0122 cm‒1
B40 = ‒ 3.7·10‒6 cm‒1, B44 = 5.6·10‒6 cm‒1

## Slide 49
Z

## Slide 50
X

## Slide 51
Y

## Slide 52
SINGLE‒CRYSTAL HFEPR SPECTRA 120 K, 218 GHz
+
gx = 1.935 gy = 1.939 gz = 1.990
D= ‒ 0.0970 cm‒1, E = ‒ 0.0122 cm‒1
B40 = ‒ 3.7 10‒6 cm‒1, B44 = 5.6 10‒6 cm‒1
Q = 10.5o

## Slide 54
RELATIONS BETWEEN THE ZFS PARAMETERS OF THE “GIANT SPIN” FOR S=11 AND THE “MICROSCOPIC” HAMILTONIAN
The ZFS parameters of the Mn(III) and Mn(IV) ions contribute to the ZFS parameters of the coupled S=11 state. In a tensor form, we have: {DS=11} = 4·(2/77){DMn(III)} + 2· (1/77) {DMn(IV)}
There is no way to determine these individual ions’ tensors in a coupled system. However, the Mn(III) and Mn(IV) ions are conservative about their ZFS. Typical values are like DMn(III) = ‒2.84 cm‒1, EMn(III) =‒0.13 cm‒1 , DMn(IV) =+0.975 cm‒1, EMn(IV) =+0.275 cm‒1.
These D and E pairs may be converted to the tensor components which are then oriented according to the S4 molecular symmetry. The above formula is applied, and the result is diagonalized leading to DS=11 = ‒0.11 cm‒1 and ES=11 = 0.

## Slide 55
CONCLUSIONS
The in‒plane and out‒of‒plane exchange integrals were determined from the magnetic susceptibility measurements
The HFEPR spectra are not in full agreement with the X‒Ray structure as the E parameter appears to be not equal to 0.
The presence of the quartic parameters and has been proven by the HFEPR spectra and the Cantilever Torque Magnetometry
Wrocław, 8 września 2025

## Slide 56: Unusual spectra of [Ni(pypz)(dca)(H2O)]n·(dca)n
[Ni(pypz)(dca)(H2O)]n·(dca)n
J. Sawka, A. Bieńko, A. Świtlicka, M. Penkalac, D. Bieńko, C. Rajnák, J. Titiš, R. Bočaf and A. Ozarowski, Dalton, in press
The parameters needed to simulate the blue traces, gx = gy = 2.18, gz = 2.19, DNi = -5.296 cm-1, ENi = -0.329 cm-1, were obtained by fitting the positions of the central resonances in the 5-line groups.

## Slide 57: Acknowledgments
NHMFL is supported by the NSF through the Cooperative Agreement No. DMR‒2128556 and the State of Florida.
LHD thanks NSF CHE‒02102532 and JEH Boston University UROP for support.
Wrocław, 8 września 2025

## Slide 58: NOTE:
Everybody can take advantage of the instrumentation of the National High Magnetic Field Laboratory
Consult https://nationalmaglab.org and
https://nationalmaglab.org/user‒resources/requesting‒magnet‒time/

## Slide 59: Thank you for your attention

## Slide 61
gx = 1.860 gy = 1.860 gz = 1.990
D= ‒ 0.0970 cm‒1, E = 0
B40 = ‒ 3.7 10‒6 cm‒1, B44 = 0
+